PART 1 GENERAL

1.01 SUMMARY

A.	Section Includes: Aluminum Storefront, including:

1. 	YKK AP Series YES 60 TU Center Set Storefront System.

B.	Related Sections:

1. 	Sealants:  Refer to Division 7 Joint Treatment Section for sealant requirements.

2. 	Glass and Glazing:  Refer to Division 8 Glass and Glazing Section for glass and glazing

requirements.

3.	Single Source Requirement:  All products listed below shall be by the same manufacturer.

a.	Section 08 32 13 Sliding Aluminum-Framed Glass Doors.

b.	Section 08 51 13 Aluminum Windows.

c.	Section 08 44 13 Glazed Aluminum Curtain Walls.

d.	Section 08 44 33 Sloped Glazing Assemblies.

1.02 	SYSTEM PERFORMANCE DESCRIPTION

A.	Performance Requirements:  Provide aluminum storefront systems that comply with performance

requirements indicated, as demonstrated by testing manufacturer's assemblies in accordance with test

method indicated.

- Air Infiltration:  Completed storefront systems shall have 0.06 CFM/FT² (1.10 m³/h•m²) maximum

allowable infiltration when tested in accordance with ASTM E 283 at differential static pressure of

6.24 PSF (299 Pa).

2. 	Water Infiltration: No uncontrolled water when tested in accordance with ASTM E 331 at test pressure differential of: 12 PSF (575 Pa) (or when required, field tested in accordance with AAMA 503).  Fastener Heads must be seated and sealed against Sill Flashing on any fasteners that penetrate through the Sill Flashing.

3. 	Wind Loads:  Completed storefront system shall withstand wind pressure loads normal to wall

plane indicated:

a. 	Exterior Walls:

1)  Positive Pressure:

2)  Negative Pressure:

b. 	Interior Walls (Pressure Acting in Either Direction):

4. 	Deflection:  Maximum allowable deflection in any member when tested in accordance with ASTM

E 330 with allowable stress in accordance with AA Specifications for Aluminum Structures.

a. 	Without Horizontals:  L/175 or 3/4" (19.1mm) maximum.

b.	With Horizontals:  L/175 or L/240 + 1/4" (6.4mm) for spans greater than 13'-6" (4.1m) 
but less than 40'-0" (12.2m).

5. Seismic: When tested in accordance with AAMA 501.4, system must meet design displacement of 0.010 x the story height and ultimate displacement no greater than 2”.

6. 	Thermal Movement:  Provide for thermal movement caused by 180 degrees F. (82.2 degrees C.)

surface temperature, without causing buckling stresses on glass, joint seal failure, undue stress on

structural elements, damaging loads on fasteners, reduction of performance, or detrimental effects.

7. 	Thermal Performance:  When tested in accordance with AAMA 507, AAMA 1503, and NFRC 100:

a. 	Condensation Resistance Factor (CRFf):  A minimum of 69 (with a CRFg of 68.)

b. 	Thermal Transmittance U Value:  0.41 BTU/HR/FT²/°F or less.

Note:  Thermal Performance for the glazed system as a whole will be affected by the characteristics of the

glass specified and percentage of vision area.

8.	Acoustical Performance: Acoustical Performance: When tested in accordance with AAMA 1801:

a.	Sound Transmission Class (STC) shall not be less than 31 for 1” standard insulating unit; 34 for

laminated glazing.

b.	Outdoor–Indoor Transmission Class (OITC) shall not be less than 25 for 1” standard insulating

unit; 29 for laminated glazing.

Note: Laminated glass based on 1” Insulated Glass Unit (1/8” / 0.030” PVB / 1/8”, ½” air space, and ¼”

annealed interior.)

1.03 	SUBMITTALS

A.	General:  Prepare, review, approve, and submit specified submittals in accordance with "Conditions of

the Contract" and Division 1 Submittals Sections. Product data, shop drawings, samples, and similar

submittals are defined in "Conditions of the Contract."

B.	Product Data:  Submit product data for each type storefront series specified.

C.  Substitutions: Whenever substitute products are to be considered, supporting technical data, samples,

and test reports must be submitted ten (10) working days prior to bid date in order to make a valid

comparison.

D.	Shop Drawings:  Submit shop drawings showing layout, profiles, and product components, including

anchorage, accessories, finish colors and textures.

E.	Samples:  Submit verification samples for colors on actual aluminum substrates indicating full color

range expected in installed system.

F.	Quality Assurance / Control Submittals:

1. 	Test Reports:  Submit certified test reports showing compliance with specified performance

characteristics and physical properties.

2. 	Installer Qualification Data:  Submit installer qualification data.

G. 	Closeout Submittals:

1. 	Warranty:  Submit warranty documents specified herein.

2. 	Project Record Documents:  Submit project record documents for installed materials in accordance

with Division 1 Project Closeout (Project Record Documents) Section.

1.04 	QUALITY ASSURANCE

A.	Qualifications:

1.	Installer Qualifications:  Installer experienced (as determined by contractor) to perform work of this

section who has specialized in the installation of work similar to that required for this project. If

requested by Owner, submit reference list of completed projects.

2. 	Manufacturer Qualifications:  Manufacturer capable of providing field service representation during

construction process.

B.	Mock-Ups (Field Constructed):  Install at project site a job mock-up using acceptable products and

manufacturer approved installation methods. Obtain Owner's and Architect's acceptance of finish color,

and workmanship standard.

1. 	Mock-Up Size:

2. 	Maintenance:  Maintain mock-up during construction for workmanship comparison; remove and

legally dispose of mock-up when no longer required.

3. 	Incorporation: Mock-up may be incorporated into final construction upon Owner's approval.

C.	Pre-Installation Meetings:  Conduct pre-installation meeting to verify project requirements, substrate

conditions, manufacturer's installation instructions, and manufacturer's warranty requirements.

1.05	PROJECT CONDITIONS / SITE CONDITIONS

A.	Field Measurements:  Verify actual measurements/openings by field measurements before fabrication;

show recorded measurements on shop drawings. Coordinate field measurements, fabrication schedule

with construction progress to avoid construction delays.

1.06	WARRANTY

A.	Project Warranty:  Refer to "Conditions of the Contract" for project warranty provisions.

B.	Manufacturer's Warranty:  Submit, for Owner's acceptance, manufacturer's standard warranty document

executed by an authorized company official.

1.	Warranty Period:  Manufacturer’s one (1) year standard warranty commencing on the substantial date of completion for the project provided that the warranty, in no event, shall start later than six (6) months from the date of shipment by YKK AP America Inc.

EDITOR NOTE:  Longer warranty periods are available at additional cost.

PART 2 PRODUCTS

2.01 	MANUFACTURERS (Acceptable Manufacturers/Products)

A.	Acceptable Manufacturers:	YKK AP America Inc.

101 Marietta Street NW, Suite 2100

Atlanta, GA 30303

Telephone: (678) 838-6000; Fax: (678) 838-6001

1. 	Storefront System: YKK AP YES 60 TU Storefront System.

B.	Storefront Framing System:

1. 	Description:  Center set, exterior flush glazed; jambs and vertical mullions continuous; head, sill,

intermediate horizontal attached by screw spline joinery or shear block attachment.

2. 	Components:  Manufacturer's standard extruded aluminum mullions, 90 degree corner posts, entrance

door framing, and indicated shapes.

3.	Thermal Barrier:  Provide continuous thermal barrier by means of a poured and debridged pocket

consisting of a two-part, chemically curing high density polyurethane which is bonded to the

aluminum by YKK ThermaBond Plus®. Systems employing non-structural thermal barriers are not

acceptable.

2.02 	MATERIALS

A.	Extrusions:  ASTM B 221 (ASTM B 221M), 6063-T5 Aluminum Alloy.

B.	Aluminum Sheet:

1.	Anodized Finish:  ASTM B 209 (ASTM B 209M), 5005-H14 Aluminum Alloy, 0.050" (1.27 mm)

minimum thickness.

2.	Painted Finish:  ASTM B 209 (ASTM B 209M), 3003-H14 Aluminum Alloy, 0.080" (1.95 mm)

minimum thickness.

2.03 	ACCESSORIES

A.	Manufacturer's Standard Accessories:

1.	Fasteners:  Zinc plated steel concealed fasteners; Hardened aluminum alloys or AISI 300 series

stainless steel exposed fasteners.

2. 	Glazing:  Setting blocks, edge blocks, and spacers in accordance with ASTM C 864, shore durometer

hardness as recommended by manufacturer; Glazing gaskets in accordance with ASTM C 864.

3.	0.050 Aluminum Sill Flashing End Dams must have 3 point attachment.

2.04 	RELATED MATERIALS (Specified In Other Sections)

A.	Glass:  Refer to Division 8 Glass and Glazing Section for glass materials.

2.05 	FABRICATION

A.	Shop Assembly:  Fabricate and assemble units with joints only at intersection of aluminum members

with uniform hairline joints; rigidly secure, and sealed in accordance with manufacturer's

recommendations.

- Hardware:  Drill and cut to template for hardware. Reinforce frames and door stiles to receive

hardware in accordance with  manufacturer's recommendations.

- Welding:  Conceal welds on aluminum members in accordance with AWS recommendations or

methods recommended by manufacturer. Members showing welding bloom or discoloration on finish

or material distortion will be rejected.

2.06 	FINISHES AND COLORS

A.  YKK AP America Anodized Plus® Finish:

CODE	DESCRIPTION

YS1N*	Clear Anodized Plus®

YH3N	Champagne Anodized Plus®

YB1N	Medium Bronze Anodized Plus®

YB5N*	Dark Bronze Anodized Plus®

YK1N*	Black Anodized Plus®

YW3N	White Anodized Plus®

M			Mill Finish

* Indicates standard finish usually carried as inventory.

Anodized Plus® is an advanced sealing technology that completely seals the anodic film yielding

superior durability (See AAMA 612).

B.	Anodized Finishing:  Prepare aluminum surfaces for specified finish; apply shop finish in accordance

with the following:

- Anodic Coating:  Electrolytic color coating followed by an organic seal applied in accordance with

the requirements of AAMA 612. Aluminum extrusions shall be produced from quality controlled

billets meeting AA-6063-T5.

a. 	Exposed Surfaces shall be free of scratches and other serious blemishes.

b. 	Extrusions shall be given a caustic etch followed by an anodic oxide treatment and then sealed

with an organic coating applied with an electrodeposition process.

c.	The anodized coating shall comply with all of the requirements of AAMA 612: Voluntary

Specifications, Performance Requirements and Test Procedures for Combined Coatings of Anodic

Oxide and Transparent Organic Coatings on Architectural Aluminum. Testing shall demonstrate

the ability of the finish to resist damage from mortar, salt spray, and chemicals commonly found

on construction sites, and to resist the loss of color and gloss.

d. 	Overall coating thickness for finishes shall be a minimum of 0.7 mils.

2) 	CASS Corrosion Resistance Test, CASS 240/ASTM B368 Test Method.

3)	Other AAMA 2605 Performance Tests specified in these specifications, such as: 7.3 Dry Film						Hardness; 7.8.2 Salt Spray Resistance; 7.9.1.2 Color Retention, South Florida; 7.9.1.4 Gloss

Retention, South Florida.

C.	High Performance Organic Coating Finish:

1.	Type Factory applied two-coat 70% Kynar resin by Arkema or 70% Hylar resin by Solvay Solexis,

fluoropolymer based coating system, Polyvinylidene Fluoride (PVF-2), applied in accordance with

YKK AP procedures and meeting AAMA 2605 specifications.

2. 	Colors: Selected by Architect from the following:

a.	Standard coating color charts.

b.	Custom coating color charts.

c.	Color Name and Number:

D.	Finishes Testing:

1.	Apply 0.5% solution NaOh, sodium hydroxide, to small area of finished sample area; leave in place

for sixty minutes; lightly wipe off NaOh; Do not clean area further.

2. 	Submit samples with test area noted on each sample.

PART 3 EXECUTION

3.01 	MANUFACTURER'S INSTRUCTIONS / RECOMMENDATIONS

A.	Compliance:  Comply with manufacturer's product data, including product technical bulletins,

installation instructions, and product carton instructions. The latest installation manual is available at

www.ykkap.com.

3.02 	EXAMINATION

A.	Site Verification of Conditions:  Verify conditions (which have been previously installed under other

sections) are acceptable for product installation in accordance with manufacturer's instructions.

3.03 	PREPARATION

A.	Adjacent Surfaces Protection:  Protect adjacent work areas and finish surfaces from damage during

product installation.

- Aluminum Surface Protection:  Protect aluminum surfaces from contact with lime, mortar, cement,

acids, and other harmful contaminants.

3.04 	INSTALLATION

A.	General:  Install manufacturer's system in accordance with shop drawings, and within specified

tolerances.

- Protect aluminum members in contact with masonry, steel, concrete, or dissimilar materials using

nylon pads or bituminous coating.

2. 	Shim and brace aluminum system before anchoring to structure.

3. 	Provide sill flashing at exterior storefront systems. Extend extruded flashing continuous with splice

joints; set in continuous beads of sealant.

4. 	Verify storefront system allows water entering system to be collected in gutters and wept to exterior.

Verify metal joints are sealed in accordance with manufacturers installation instructions.

5. 	Locate expansion mullions where indicated on reviewed shop drawings.

6. 	Seal metal to metal storefront system joints using sealant recommended by system manufacturer.

3.05	 FIELD QUALITY CONTROL

A.	Manufacturer's Field Services:  Upon request, provide manufacturer's field service consisting of site visit

for inspection of product installation in accordance with manufacturer's instructions.

B. 	Field Test:  Conduct field test to determine watertightness of storefront system. Conduct test in

accordance with AAMA 501.2.

3.06 	ADJUSTING AND CLEANING

A.	Adjusting:  Adjust swing doors for operation in accordance with manufacturer's recommendations.

B.	Cleaning:  The General Contractor shall clean installed products in accordance with manufacturer's

instructions prior to owner's acceptance, and remove construction debris from project site. Legally

dispose of debris.

C.	Protection:  The General Contractor shall protect the installed product's finish surfaces from damage

during construction.

END OF SECTION

This document supersedes all previous versions.